Supplemental material

| a) | b) |
| --- | --- |
| c) |  |

Figure S1. a) and b) Bright-field, and c) dark-field TEM images of the TNZT with 1 wt.% of TiB2 processed by L-PBF. Figure a) and c) show more details of the TiB formed in the interdendritic region. Figure b) shows a high density of dislocations inside and outside some dendrites.