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Figure S1. a) and b) Bright-field, and c) dark-field TEM images of the TNZT with 1 wt.% of TiB2 processed by L-PBF. Figure a) and c) show more details of the TiB formed in the interdendritic region. Figure b) shows a high density of dislocations inside and outside some dendrites.

23

image1.png
100 nm





image2.png




image3.png




