Supporting information for

A Novel Iron(III)-Based MOF: Synthesis, Characterization, Biological, and Antimicrobial Activity Study

Sheta M. Sheta1, *, Salem R. Salem2, Said M. El-Sheikh 3

1 Department of Inorganic Chemistry, National Research Centre, 33, El-Behouth St., Dokki, Giza, 12622, Egypt.

2 Biochemistry Department, Egypt Centre for Research and Regenerative Medicine, Cairo, 11887, Egypt.

3 Nanomaterials and Nanotechnology Department, Central Metallurgical R & D Institute, Cairo, 11421, Egypt.

*Corresponding author

Sheta, M. Sheta, E-mail: dr.sheta.nrc@gmail.com, Tel.: +20 1009697356, Fax: +2-02-33370931.

Fig. S1: The proposed mechanism of the Fe(III)-MOF synthesis.

Fig. S2: The mass spectrum of the Fe(III)-MOF (Inside proposed fragmentation Scheme).

Fig. S3: The 1H-NMR spectrum of the Fe(III)-MOF.

Fig. S4: The 13C-NMR spectrum of the Fe(III)-MOF.

Fig. S5: The X-ray photoelectron spectroscopic analysis (XPS) of Fe(III)-MOF: O 1s deconvolution fitting.

Fig. S6: The X-ray photoelectron spectroscopic analysis (XPS) of Fe(III)-MOF: N 1s deconvolution fitting.

Fig. S7: The X-ray photoelectron spectroscopic analysis (XPS) of Fe(III)-MOF: C 1s deconvolution fitting

Fig. S8:	The BET surface area analysis of Fe(III)-MOF: N2 adsorption/desorption isotherm.

Fig. S9:	The BET surface area analysis of Fe(III)-MOF: Changes in pore volume distribution in relation to pore radius.

Fig. S10: The photoluminescence spectrum emission band after excitation at 384 nm of the Fe(III)-MOF.

Fig. S11: The magnetization curve of the Fe(III)-MOF.

Table S1: EDX analysis of the Fe(III)-MOF.

| Element | Weight % | Atomic % | Net Int. | Error % |
| --- | --- | --- | --- | --- |
| C | 49.65 | 56.51 | 125.01 | 8.82 |
| N | 9.18 | 8.96 | 12.32 | 17.86 |
| O | 20.20 | 17.26 | 35.19 | 13.95 |
| Fe | 20.97 | 17.27 | 10.89 | 4.11 |

Table S2: XPS Survey scans

| Name | Peak BE | FWHM, eV | Area (P) CPS., eV | Atomic, % |
| --- | --- | --- | --- | --- |
| C1s | 284.09 | 3.44 | 156525.1 | 56.27 |
| O1s | 531.14 | 3.8 | 170091.3 | 17.12 |
| N1s | 398.79 | 3.74 | 31509.33 | 8.61 |
| Fe2p | 710.69 | 6.45 | 45405.55 | 18.00 |