Supporting Information

Effect of structural iron on nanoscroll formation via exfoliation of a high-iron content kaolin

Balázs Zsirka1*, Katalin Győrfi1, Takahide Yamaguchi2, Attila Táborosi3, Veronika Vágvölgyi1, Clara Parameswary4, Zoltán Homonnay4, Ernő Kuzmann4, Erzsébet Horváth1, János Kristóf1

1 Research Group of Analytical Chemistry/Laboratory for Surfaces and Nanostructures, University of Pannonia, P.O. Box 158, Veszprém 8201, Hungary

2  Institute of Quantum Beam Science, Graduate School of Science and Engineering, Ibaraki University, 2-1-1, Bunkyo, Mito, Ibaraki 310-8512, Japan

3  Research Initiative for Supra-Materials, Faculty of Engineering, Shinshu University, 4-17-1, Wakasato, Nagano city, Nagano 380-8853, Japan

4 Institute of Chemistry, ELTE Eötvös Loránd University, Pázmány Péter s. 1/A, Budapest, 1117, Hungary

Table of Contents:

Figure S1. Resolved XRD patterns of nKao and 11M-nKao samples and of their oxidative surface treated derivatives.	2

Table S1. Full width at half maxima (FWHM), average crystallite size (d) and the average number adjoined TO layers (N) of kaolinite, as calculated by the Scherrer equation [1].	3

Figure S2. FTIR-ATR spectra of Kao (a) and 11M-Kao (a2) samples, intercalated with (b) potassium acetate, (c) ethylene-glycol, (d) hexylamine, (e) toluene, and after surface cleaning with (f) 2-propanol, acetone and water, (g) hydrogen-peroxide in the 4000-400 cm-1 range.	4

Table S2. Elemental composition determined by STEM-EDX from the designated areas of Figure 4. Values of Fe are highlighted.	5

Table S3. Mössbauer parameters of pristine sample Kao at room temperature and at 80 K. Fitted errors are given in brackets.	6

Figure S3. Fe K-edge XANES of Kao (solid line) compared to the simulated XANES by mixing Hematite and Goethite spectra (dashed lines). Mixing ratio of Hematite:Geothite were (A) 0.1:0.9, (B) 0.2:0.8, (C) 0.3:0.7, (D) 0.4:0.6, (E) 0.5:0.5, (F) 0.6:0.4, (G) 0.7:0.3, (H) 0.8:0.2, (I) 0.9:0.1.	7

Figure S4. The first derivative of Fe K-edge XANES region of the Kao (black), 5M-Kao (orange), 11M-Kao (red) samples compared to and the FeO (purple), hematite (blue), and goethite (green).	7

Figure S5. Fe K-edge EXAFS of Kao (black), 5M-Kao (orange), and 11M-Kao (red) clays compared to and the hematite (blue), and goethite (green) in k-space	8

Figure S6. Fe K-edge EXAFS of hematite (blue), goethite (green), and 11M-Kao with fitting curves (black, dashed) in R-space.	9

Figure S7. The Generation 2 (G2) molecular cluster model for nano-kaolinite (A), the replacement positions of Al3+ to Fe3+/Fe2+, and the inner coordinates of Fe3+/Fe2+. The designations of sHO-, aO2- and iHO- indicates the surface-hydroxide, apical-oxide and inner-hydroxide groups, respectively.	10

Table S4. Comparison of the first and second shell distances and their averages of the three different positions (Figure S7. P1, P2, P3) for Al3+, Fe3+ and Fe2+ for both high and low spin states.	11

Table S5. Calculated energies (E), their comparison (ΔE) and the Boltzmann distribution values at 298K.	11

References	12

## Figure S1. Resolved XRD patterns of nKao and 11M-nKao samples and of their oxidative surface treated derivatives.

## Table S1. Full width at half maxima (FWHM), average crystallite size (d) and the average number adjoined TO layers (N) of kaolinite, as calculated by the Scherrer equation [1].

| Sample | Kaolinite (001) |  |  |
| --- | --- | --- | --- |
|  | FWHM (°) | d(nm) | Number of TO layers |
| Kao | 0.186 | 345.6 | 480 |
| nKao (whole range, 1 peak) | 1.165 | 8.0 | 11 |
| nKao (deconvoluted, 3 peaks) | 0.951 | 10.1 | 14 |
|  | 0.905 | 10.8 | 15 |
|  | 0.246 | 95.9 | 133 |
| nKao (H2O2) (whole range, 1 peak) | 1.180 | 7.9 | 11 |
| nKao (H2O2) (deconvoluted, 3 peaks) | 0.552 | 20.5 | 28 |
|  | 1.081 | 8.7 | 12 |
|  | 0.239 | 105.5 | 146 |
| 11M-Kao | 0.186 | 340.5 | 473 |
| 11M-nKao (whole range, 1 peak) | 1.848 | 4.7 | 7 |
| 11M-nKao (deconvoluted, 3 peaks) | 0.822 | 12.1 | 17 |
|  | 1.371 | 6.6 | 9 |
|  | 0.375 | 37.8 | 52 |
| 11M-nKao (H2O2) (whole range, 1 peak) | 1.864 | 4.7 | 7 |
| 11M-nKao (H2O2) (deconvoluted, 3 peaks) | 0.770 | 13.1 | 18 |
|  | 1.391 | 6.5 | 9 |
|  | 0.434 | 29.5 | 41 |

## Figure S2. FTIR-ATR spectra of Kao (a) and 11M-Kao (a2) samples, intercalated with (b) potassium acetate, (c) ethylene-glycol, (d) hexylamine, (e) toluene, and after surface cleaning with (f) 2-propanol, acetone and water, (g) hydrogen-peroxide in the 4000-400 cm-1 range.

## Table S2. Elemental composition determined by STEM-EDX from the designated areas of Figure 4. Values of Fe are highlighted.

| #### Sample |  | #### Element | #### Atom% | #### Mass% |
| --- | --- | --- | --- | --- |
| #### nKao | #### Figure 4/a | #### O | #### 66.65 ± 6.44 | #### 50.01 ± 3.06 |
|  |  | #### Al | #### 6.79 ± 1.49 | #### 8.59 ± 1.78 |
|  |  | #### Si | #### 21.57 ± 4.64 | #### 28.42 ± 5.73 |
|  |  | #### Ti | #### 0.2 ± 0.03 | #### 0.46 ± 0.07 |
|  |  | #### Fe | #### 4.78 ± 0.78 | #### 12.53 ± 1.83 |
|  | #### Figure 4/b | #### O | #### 70.11 ± 2.31 | #### 55.69 ± 0.77 |
|  |  | #### Al | #### 12.94 ± 3.08 | #### 17.33 ± 3.38 |
|  |  | #### Si | #### 14.54 ± 3.41 | #### 20.26 ± 3.87 |
|  |  | #### Ti | #### 0.09 ± 0.02 | #### 0.21 ± 0.03 |
|  |  | #### Fe | #### 2.34 ± 0.47 | #### 6.5 ± 0.96 |
| #### 11M-nKao | #### Figure 4/c | #### O | #### 69.23 ± 6.61 | #### 56.31 ± 3.42 |
|  |  | #### Al | #### 12.67 ± 2.78 | #### 17.38 ± 3.59 |
|  |  | #### Si | #### 17.75 ± 3.81 | #### 25.34 ± 5.11 |
|  |  | #### Ti | #### 0.11 ± 0.02 | #### 0.26 ± 0.04 |
|  |  | #### Fe | #### 0.25 ± 0.04 | #### 0.71 ± 0.1 |
|  | #### Figure 4/d | #### O | #### 70.58 ± 6.54 | #### 57.99 ± 3.45 |
|  |  | #### Al | #### 14.03 ± 3.06 | #### 19.44 ± 4 |
|  |  | #### Si | #### 15.11 ± 3.22 | #### 21.79 ± 4.38 |
|  |  | #### Ti | #### 0.06 ± 0.01 | #### 0.14 ± 0.02 |
|  |  | #### Fe | #### 0.22 ± 0.04 | #### 0.65 ± 0.09 |

## Table S3. Mössbauer parameters of pristine sample Kao at room temperature and at 80 K. Fitted errors are given in brackets.

|  | room temperature |  |  |  |  | 80K |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Mössbauer parameters | hematite | goethite | Fe3+ | Fe2+ | hematite |  | goethite | Fe3+ | Fe2+ |
| Relative area (%) | 28.7 (±0.7) | 58.1 (±6,5) | 11.6 (±0.5) | 1.6 (±0,4) | 18.2 (±2.6) |  | 73.8 (±3.6) | 5.7 (±0.7) | 2.4 (±1.1) |
| Isomer shift (mm/s) | 0.382 (±0.005) | 0.35 (±0.03) | 0.34 (±0.01) | 1.35 (±0.03) | 0.49 (±0.01) |  | 0.487 (±0.005) | 0.43 (±0.04) | 1.15 (±0.13) |
| Quadrupole splitting/shift (mm/s) | -0.217 (±0.009) | -0.27 (±0.05) | 0.59 (±0.02) | 2.31 (±0.35) | -0.14 (±0.02) |  | -0.23 (±0.01) | 0.68 (±0.06) | 2.76 (±0.26) |
| Hyperfine magnetic field (T) | 49.4 (±0.04) | 29.4 (±0.3) | N/A | N/A | 52.69 (±0.09) |  | 48.95 (±0.08) | N/A | N/A |
| Line width/range* (mm/s) | 0.35-0.66 | 0.63-2.72 | 0.50 (±0.04) | 0.35 (±0.10) | 0.38-0.40 |  | 0.43-0.80 | 0.54 (±0.10) | 0.72 (±0.42) |

*The sextets for goethite and hematite were analyzed with variable line widths for the 1-6, 2-5 and 3-4 pairs of lines. The observed line width ranges are given.

## Figure S3. Fe K-edge XANES of Kao (solid line) compared to the simulated XANES by mixing Hematite and Goethite spectra (dashed lines). Mixing ratio of Hematite:Geothite were (A) 0.1:0.9, (B) 0.2:0.8, (C) 0.3:0.7, (D) 0.4:0.6, (E) 0.5:0.5, (F) 0.6:0.4, (G) 0.7:0.3, (H) 0.8:0.2, (I) 0.9:0.1.

## Figure S4. The first derivative of Fe K-edge XANES region of the Kao (black), 5M-Kao (orange), 11M-Kao (red) samples compared to and the FeO (purple), hematite (blue), and goethite (green).

## Figure S5. Fe K-edge EXAFS of Kao (black), 5M-Kao (orange), and 11M-Kao (red) clays compared to and the hematite (blue), and goethite (green) in k-space

## Figure S6. Fe K-edge EXAFS of hematite (blue), goethite (green), and 11M-Kao with fitting curves (black, dashed) in R-space.

## Figure S7. The Generation 2 (G2) molecular cluster model for nano-kaolinite (A), the replacement positions of Al3+ to Fe3+/Fe2+, and the inner coordinates of Fe3+/Fe2+. The designations of sHO-, aO2- and iHO- indicates the surface-hydroxide, apical-oxide and inner-hydroxide groups, respectively.

## Table S4. Comparison of the first and second shell distances and their averages of the three different positions (Figure S7. P1, P2, P3) for Al3+, Fe3+ and Fe2+ for both high and low spin states.

|  |  | Al/Fe-O, Å |  |  |  | Al/Fe—Al, Ave. Å | Al/Fe—Si, Ave. Å |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Al/Fe-sHO- | Al/Fe-iHO- | Al/Fe-aO2- | Ave. |  |  |
| Al3+ | P1 | 1.89 | 1.92 | 1.97 | 1.92 | 2.93 | 3.25 |
|  | P2 | 1.92 | 1.92 | 1.96 | 1.92 | 2.92 | 3.25 |
|  | P3 | 1.92 | 1.91 | 1.95 | 1.92 | 2.91 | 3.25 |
| Fe3+ | high spin |  |  |  |  |  |  |
|  | P1 | 2.00 | 2.04 | 2.12 | 2.05 | 3.04 | 3.35 |
|  | P2 | 2.00 | 2.05 | 2.10 | 2.04 | 3.03 | 3.35 |
|  | P3 | 2.01 | 2.04 | 2.08 | 2.04 | 3.02 | 3.34 |
|  | low spin |  |  |  |  |  |  |
|  | P1 | 1.92 | 1.96 | 2.01 | 1.95 | 2.95 | 3.24 |
|  | P2 | 1.91 | 1.97 | 1.99 | 1.95 | 2.95 | 3.24 |
|  | P3 | 1.92 | 1.96 | 1.98 | 1.95 | 2.94 | 3.24 |
| Fe2+ | high spin |  |  |  |  |  |  |
|  | P1 | 2.09 | 2.11 | 2.25 | 2.15 | 3.05 | 3.38 |
|  | P2 | 2.09 | 2.14 | 2.21 | 2.14 | 3.03 | 3.37 |
|  | P3 | 2.10 | 2.12 | 2.20 | 2.14 | 3.01 | 3.37 |
|  | low spin |  |  |  |  |  |  |
|  | P1 | 2.06 | 2.02 | 2.11 | 2.06 | 2.95 | 3.25 |
|  | P2 | 2.01 | 2.02 | 2.06 | 2.03 | 2.91 | 3.21 |
|  | P3 | 2.01 | 2.02 | 2.04 | 2.02 | 2.90 | 3.22 |

*The inner coordinates result for Al3+ were taken from a previous study of nano kaolinite [2].

## Table S5. Calculated energies (E), their comparison (ΔE) and the Boltzmann distribution values at 298K.

|  |  |  | E, a.u. | ΔE, kJ/mol | Boltzmann % (at 298K) |
| --- | --- | --- | --- | --- | --- |
| Fe3+ | high spin | P1 | -35146.0044 | 0 | 67% |
|  |  | P2 | -35146.0031 | 3 | 16% |
|  |  | P3 | -35146.0018 | 7 | 4% |
|  | low spin | P1 | -35146.0017 | 7 | 3% |
|  |  | P2 | -35146.0021 | 6 | 6% |
|  |  | P3 | -35146.0019 | 7 | 4% |
| Fe2+ | high spin | P1 | -35146.1465 | 0 | 98% |
|  |  | P2 | -35146.1426 | 10 | 1% |
|  |  | P3 | -35146.1413 | 14 | 0% |
|  | low spin | P1 | -35146.1204 | 68 | 0% |
|  |  | P2 | -35146.1156 | 81 | 0% |
|  |  | P3 | -35146.1151 | 82 | 0% |

# References

[1]	Patterson AL. The Scherrer Formula for X-Ray Particle Size Determination. Phys Rev 1939;56:978–82. https://doi.org/10.1103/PhysRev.56.978.

[2]	Táborosi A, Szilagyi RK, Zsirka B, Fónagy O, Horváth E, Kristóf J. Molecular treatment of nano-kaolinite generations. Inorg Chem 2018;57:7151–67. https://doi.org/10.1021/acs.inorgchem.8b00877.