Supplemental Information for

# Molten flux growth of single crystals of quasi-1D hexagonal chalcogenide BaTiS3

# Authors: Huandong Chen1, Shantanu Singh1, Hongyan Mei2, Guodong Ren3, Boyang Zhao1, Mythili Surendran1,4, Yan-Ting Wang1, Rohan Mishra5,3, Mikhail A. Kats2,6, Jayakanth Ravichandran1,4,7*

1Mork Family Department of Chemical Engineering and Materials Science, University of Southern California, Los Angeles CA, USA

2Department of Electrical and Computer Engineering, University of Wisconsin-Madison, Madison WI, USA

3Institute of Materials Science & Engineering, Washington University in St. Louis, St. Louis MO, USA

4Core Center for Excellence in Nano Imaging, University of Southern California, Los Angeles CA, USA

5Department of Mechanical Engineering and Materials Science, Washington University in St. Louis, St. Louis MO, USA

6Department of Materials Science and Engineering, University of Wisconsin-Madison, Madison WI, USA

7Ming Hsieh Department of Electrical and Computer Engineering, University of Southern California, Los Angeles CA, USA

*Email: j.ravichandran@usc.edu

Figure S1. (a) Elemental edge maps using Ba-M, Ti-L, and S-L edges extracted from an EELS image. (b) The EEL spectra of the corresponding elements used to make the elemental maps in (a). The energy range used for signal integration have been highlighted with shaded boxes.

Figure S2. Optical images of quartz ampoules prepared for (a) KI flux growth, and (b) BaCl2-BaI2 flux growth. Additional alumina crucible was used as inner container for BaCl2-BaI2 flux to minimize its corrosion to quartz ampule.

Figure S3. Optical images of several different steps of BaTiS3 crystal synthesis using KI flux: (a) after sealing KI flux, pre-synthesized BaTiS3 powder and excess sulfur in a quartz ampule, (b) after loading samples in an alumina crucible, (c) after sealing alumina crucibles using high temperature cement, this step protects the furnace from any potential leaking, and (d) removing excess KI flux in a crystallizing dish using DI water.

Figure S4. (a) Precession maps of a conventional CVT-grown BaTiS3 crystal along hk2 projection for three different phases. The data was adapted from the Reference1. (b) Reciprocal precession images of a BaCl2-BaI2 flux-grown BaTiS3 crystal along the same projection, taken at 300 K, 220 K, and 100 K, respectively during the warming cycle.

Table S1.  Evolution of flux-grown BaTiS3 unit cell sizes at different temperatures

| Flux-BaTiS3 | 300 K | 240 K | 100 K |
| --- | --- | --- | --- |
| a, b, c (Å) | 11.71, 11.71, 5.84 | 23.38, 23.38, 5.85 | 13.46, 13.46, 5.83 |
|  () | 90, 90, 120 | 90, 90, 120 | 90, 90, 120 |
| space group | P63cm | P3c1 | P21 |

Figure S5. (a) optical images of a KI flux grown BaTiS3 crystal plate, with dimension along the c-axis larger than 1.8 mm. (b) cross-section image of a KI flux grown BaTiS3 crystal plate, showing the thickness of ~255 µm.

Figure S6. Raw ellipsometry data (Ψ (a-c) and Δ (d-f) of Ane, Mueller matrix elements (g-i)) for KI flux grown BaTiS3 at θi=55° with the crystal c-axis perpendicular, parallel, and at an off-axis angle ~48° to the plane of incidence, showing good consistence between the experimental data (green lines) and model fit data (red lines).

Figure S7. The ε2 values calculated from the final optical oscillator model used to fit to the ellipsometry data of KI flux grown BaTiS3. The optical oscillator model is built on Kramers-Kronig consistent oscillators.

Figure S8. Infrared transmission spectra of a thick KI flux-grown BaTiS3 crystal with incident light polarized at 0˚ and 90˚, with respective to the c-axis. No substantial difference was observed between different polarizations and the absolute values of transmittances are low. Two different objective lenses (15, NA = 0.4, Casegrain reflective objective; 5, NA = 0.17, Ge IR refractive objective) have been used for the measurements. The corresponding reflectance spectra with NA = 0.4 is shown in Figure 3a.

Figure S9. Infrared transmission spectra of a relatively thin KI flux-grown BaTiS3 crystal (~ 40 µm thick) with incident light polarized perpendicular and parallel to the c-axis. Two absorption edges at ~ 0.35 eV and ~ 0.77 eV are clearly revealed. Energy scale was used for the ease of analysis.

Supplementary Note 1. Extraction of the Anisotropic Complex Refractive Index

Generalized spectroscopic ellipsometry (VASE + focusing optics, J.A. Woollam Co.) and polarized reflection/transmission infrared spectroscopy (Bruker VERTEX 70 + Hyperion 2000 with MCT IR detector) were employed to extract the complex refractive index tensor of KI flux grown BaTiS3 from 210 nm to 17 µm. The BaTiS3 crystal was suspended over air with no substrate during the measurement, as shown in Figure S5.

Four ellipsometry measurements were made under Mueller Matrix Mode with three different crystal orientations: with the crystal c-axis perpendicular to the plane of incidence; parallel to the plane of incidence; and at off-axis angles (~48°) and the three measurements were made with an angle of incidence of 55° from the surface normal.

Figure S6 shows the fitting between the raw measured ellipsometry data (in green) and the corresponding model data (in red) for the three measurements of KI flux grown BaTiS3, consisting of the generalized ellipsometry data types Ane and Mueller matrix elements mm12, …,mm34. Ane is the ratio between the two Fresnel coefficients rpp and rss. Mueller matrix elements describe how the sample transforms the Stokes vector of the incident light. The m11 element represents the total intensity of the reflection or transmission of the sample and the VASE ellipsometer records other Mueller matrix elements normalized to m11, so the quantities range between -1 and +12.

Ane=ρ=rpprss=tanΨAneeiΔAne

S=IQUV=MIinQinUinVin,   M=m11m12m13m14m21m22m23m24m31m32m33m34m41m42m43m44=m111m12'm13'm14'm21'm22'm23'm24'm31'm32'm33'm34'm41'm42'm43'm44'

All three datasets were fitted simultaneously using a single optical model with uniaxial birefringence. Here, optical properties perpendicular and parallel to the c-axis contain independent oscillators. By integrating the polarization-resolved reflectance of KI flux grown BaTiS3 into the ellipsometry data, the optical model could be extended up to the detection limit of our FTIR (17 μm). Thus, three ellipsometry measurements and two reflectance measurements could all be fit simultaneously to a single anisotropic optical model to yield a full set of refractive indices spanning 210 nm through 17 μm. As shown in Figure S6, the measured data match well with the model fitted data.

The total oscillator model for each direction is the sum of individual Kramers-Kronig-consistent oscillators as shown in Figure S7. Table S2 lists the oscillators used in the anisotropic optical model for both the ordinary and extraordinary directions.

Table S2. Oscillators and the fitted parameters of KI flux grown BaTiS3.

| Oscillator | Parameters (eV) |  |  |
| --- | --- | --- | --- |
| Gaussian εGaus=ε1+iε2 ε2=Ane-E-Enσ2-Ane-E+Enσ2 ε1 =2πP0∞ξε2(ξ)ξ2-E2dξ Where σ=Brn2ln2, the 1/2In(2) factor defines Brn=FWHM. P is the Cauchy Principal Value. | Ordinary A1 = 0.22881 A2 = 1.7844 A3 = 0.10508 A4 = 0.11355 A5 = 2.117 A6 = 0.67282 A7 = 0.19641 A8 = 3.0509 A9 = 0.44297 Extraordinary A1 = 0.49005 A2 = 6.0344 A3 = 2.1032 A4 = 9.455 A5 = 0.47327 A6 = 3.0859 A7 = 5.616 A8 = 3.4602 A9 = 1.0241 A10 = 2.3982 A11 = 1.2056 A12 = 0.85088 A13 = 0.84736 A14 = 0.24468 A15 = 1.3047 | Ordinary E1 = 1.1236 E2 = 1.4476 E3 = 1.5034 E4 = 2.3794 E5 = 2.5385 E6 = 3.4884 E7 = 3.5532 E8 = 4.6747 E9 = 5.5807 Extraordinary E1 = 0.29574 E2 = 0.5 E3 = 0.70144 E4 = 1.0952 E5 = 1.5367 E6 = 1.5826 E7 = 2.2017 E8 = 2.3637 E9 = 2.7584 E10 = 3.2084 E11 = 3.7787 E12 = 4.4721 E13 = 5.0477 E14 = 5.7131 E15 = 6.0456 | Ordinary Br1 = 0.4612 Br2 = 0.73465 Br3 = 0.27766 Br4 = 0.23803 Br5 = 0.97834 Br6 = 1.1235 Br7 = 0.91346 Br8 = 3.3703 Br9 = 0.36085 Extraordinary Br1 = 0.31132 Br2 = 0.3465 Br3 = 0.24885 Br4 = 0.56054 Br5 = 0.32465 Br6 = 0.445 Br7 = 0.49401 Br8 = 0.5914 Br9 = 0.5183 Br10 = 0.91344 Br11 = 1.0342 Br12 = 0.79528 Br13 = 0.69215 Br14 = 0.86262 Br15 = 2.6429 |
| Lorentz εL=ε1+iε2 ε2= AnBrnEnEn2-E2-iBrnE ε1 =2πP0∞ξε2(ξ)ξ2-E2dξ Where P is the Cauchy Principal Value. | Ordinary A1 = 3.3693 E1 = 2.1165 Br1 = 0.64235 |  |  |
| Parametric Semiconductor Psemi-(M0, M1, M2, M3 & Tri) See WVASE manual by J.A. Woollam Co.2 | Ordinary (Psemi-Tri) |  |  |
|  | A1 = 1.7299 | Ec1 = 1.233 | B1 = 0.18861 |
|  | WL1 = 1.0042 WR1 = 1.0207 |  |  |
|  | AL1 = 0.86247 AR1 = 0.1880 |  |  |

Reference

1	Chen, H. et al. Charge density wave order and electronic phase transitions in a dilute d-band semiconductor. Adv. Mater., 2303283 (2023).

2	Woollam, J. Guide to Using WVASE: Spectroscopic Ellipsometry Data Acquisition and Analysis Software: Lincoln. NE, USA: JA Woollam Company, Incorporated (2012).