Supporting information

Torsional Performance and Failure Analysis of FFF Carbon Fiber–Reinforced PLA: An  Experimental Study

Muhammad Haseem Umer,a,b Muhammad Bilal Khanc*, Muhammad Qasim Zafard, Ghulam Hussaind, Muhammad Hassan Razzaqe,f,g*

*Correspondence Author: Muhammad Hassan Razzaq (razzaq@mci.sdu.dk)

Muhammad Bilal Khan (muhammadbilalkhan@zju.edu.cn)

aFaculty of Mechanical Engineering, Ghulam Ishaq Khan Institute of Engineering Sciences and Technology, Topi, Swabi, 23640, KP, Pakistan.

bDepartment of Mechanical and Aerospace Engineering, Air University, Islamabad, 44000, Pakistan.

cMechanical Engineering Department, College of Engineering, University of Bahrain, Isa Town, 32038, Bahrain.

dDepartment of Civil Engineering, Zhejiang University, Hangzhou, 310058, China

eDepartment of Mechanical Engineering, Institute for Graduate School of Natural and Applied Sciences, Gazi University, Ankara 06570, Türkiye.

fAdditive Manufacturing Technologies Application and Research Center - EKTAM, Gazi University, 06980, Kahramankazan, Ankara, TÜRKIYE.

gSmart Materials, NanoSYD, Mads Clausen Institute, University of Southern Denmark, Alsion 2, 6400, Sønderborg, Denmark

Figure S1: Fit measuring criteria: (a) Shear modulus; (b) Yield strength; (c) Ultimate shear strength; (d) Failure strain; [(i) Normal distribution plot; (ii) Actual and predicted plot; and (iii) Box-cox plot.

Table S1: Shear properties from torsion testing of samples.

| Sample | Shear Modulus (MPa) | Yield Stress (MPa) | Ultimate Shear Stress (MPa) | Failure Strain (%) |
| --- | --- | --- | --- | --- |
| 1 | 176.29 | 3.83 | 5.35 | 14.58 |
| 2 | 653.58 | 9.87 | 10.89 | 14.56 |
| 3 | 597.68 | 13.60 | 15.40 | 11.85 |
| 4 | 292.39 | 8.42 | 9.63 | 12.53 |
| 5 | 176.29 | 6.47 | 7.26 | 14.40 |
| 6 | 438.59 | 10.72 | 11.63 | 13.21 |
| 7 | 440.74 | 10.89 | 11.77 | 13.29 |
| 8 | 436.44 | 10.59 | 11.56 | 13.13 |
| 9 | 741.73 | 15.25 | 16.26 | 11.56 |
| 10 | 438.59 | 10.68 | 11.63 | 13.20 |
| 11 | 219.29 | 7.969 | 9.76 | 11.83 |
| 12 | 445.04 | 12.99 | 16.78 | 10.84 |
| 13 | 126.84 | 3.08 | 4.04 | 14.66 |
| 14 | 879.33 | 17.35 | 18.90 | 7.85 |
| 15 | 438.59 | 10.16 | 11.63 | 13.18 |
| 16 | 705.18 | 10.68 | 11.90 | 14.51 |
| 17 | 761.08 | 12.20 | 15.22 | 14.20 |
| 18 | 292.39 | 11.92 | 15.85 | 8.46 |
| 19 | 437.51 | 5.573 | 6.432 | 13.96 |