Supplementary Information

Mastering Binder Jet 3D Printing of 316L Stainless Steel: A Descriptive Model Approach to Particle Size and Deposition Thickness

A. Simchi1,2*, B. Barthel1, S.B. Hein1, L. Reineke1, D. Hosseini2

1Fraunhofer Institute for Manufacturing Technology and Advanced Materials (IFAM), 28359 Bremen, Germany

2Department of Materials Science and Engineering, Sharif University of Technology, 14588 Tehran, Iran

*Corresponding author: abdolreza.simchi@ifam.fraunhofer.de (A. Simchi)

Fig. S1. (a) Particle size distribution of 316 SS powders. Representative SEM images of selected powders showing the spherical morphology of the particles: (b) 10 µm; (c) 16 µm; (d) 22 µm.

Fig. S2. Representative images of printed (a) cuboidal parts (1 cm3) and (b) cups (Outer diameter: 35 mm)

Table S1. Parameters used for binder jet additive manufacturing of 316L powders

| Parameter | Value |
| --- | --- |
| Droplet/line spacing, µm | X= 50.8; Y=51 |
| Print head traverse velocity, mm.s-1 | 150 |
| Print passes per X jet spacing | 5 |
| Droplet volume, pL | 26 |
| Droplet frequency, Hz | 2900 |
| Roller transverse speed, mm.min-1 | 5 |
| Roller rotational speed, U.min-1 | 500 |
| Roller diameter, mm | 12 |
| Binder saturation, % | 65 |
| Foundation layer | 10 |
| Bottom bleed reduction, % | 50 |
| Z-Retraction, mm | 0.1 |
| Bed temperature, °C | 40 |