### Supplementary Information

- Changed the title.

- This assumption is also confirmed by data on dynamic light scattering in samples (Figure 3). Small decrease in zeta potential should also be noted (Table 1)

(b)

(b)

(a)

(a)

(c)

(c)

Figure 1. Size of BaTiO3-OH nanoparticles modified with (a) 1, (b) 2 and (c) 3 (%v/v) hydrolyzed chitosan

Table 1. Average size and Z potential values of BaTiO3-OH nanoparticles modified with (a) 1, (b) 2 and (c) 3 (%v/v) hydrolyzed chitosan

| Sample | Average size (nm) | Z potential (mV) |
| --- | --- | --- |
| BaTiO3@CH1 | 314.2 0.1 | 14.34 0.70 |
| BaTiO3@CH1 | 287.5 0.1 | 13.66 0.22 |
| BaTiO3@CH1 | 220.4 0.1 | 12.36 0.69 |

- Stability of BaTiO3-OH nanoparticles modified with 3 (%v/v) hydrolyzed chitosan

Day 1: 04/07/2022

Day 2: 04/08/2022

Day 3: 04/09/2022:

Figure 2. Stability of BaTiO3-OH nanoparticles modified with 3 (%v/v) hydrolyzed chitosan