
Supplementary Information
1. Changed the title.



2. This assumption is also confirmed by data on dynamic light scattering in samples (Figure 3). Small decrease in zeta potential should also be noted (Table 1)

[image: ][image: ](b)
(a)




[image: ](c)




Figure 1. Size of BaTiO3-OH nanoparticles modified with (a) 1, (b) 2 and (c) 3 (%v/v) hydrolyzed chitosan


Table 1. Average size and Z potential values of BaTiO3-OH nanoparticles modified with (a) 1, (b) 2 and (c) 3 (%v/v) hydrolyzed chitosan
	Sample
	Average size (nm)
	Z potential (mV)

	BaTiO3@CH1
	314.2 0.1
	14.34  0.70

	BaTiO3@CH1
	287.5 0.1
	13.66  0.22

	BaTiO3@CH1
	220.4 0.1
	12.36  0.69
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Figure 2. Stability of BaTiO3-OH nanoparticles modified with 3 (%v/v) hydrolyzed chitosan
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