Supplementary Material

Detection of Acetone Vapours Using Solution-Processed Tin Oxide Thin-Film Transistors

Lauren R. Miller 1, Robert J. Borthwick1, Paloma L. dos Santos1, and Mujeeb U. Chaudhry 1

1 Department of Engineering, Durham University

Lower Mountjoy, South Rd, Durham DH1 3LE

(a)

(b)

(a)

(b)

Fig. S1. (a) Output characteristics for TFTs annealed at 350 °C and; (b) 450 °C at Vgs = 0 to 40 V in steps of 5 V and L = 50 μm.

(a)

(b)

(a)

(b)

Fig. S2. (a) XRD analysis of TFT annealed at 350 °C for 2θ = 5 to 60 °; (b) AFM image of TFT annealed at 350 °C with 2 μm scan area.

Table S1. Current on/off ratio (Ion/off), maximum leakage current (Igs[max]), μeff, Ids [max] and Vth of SnO2 TFTs annealed at 350 °C and 450 °C for L = 50, 80, 100 and 120 μm before exposure, after exposure, and recovery.

| T (̊ C) |  |  | L (μm) | μeff (cm2V-1s-1) | Ion/off | Ids [max] (A) | Igs [max] (A) | Vth (V) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 450 | As prepared |  | 50 | 0.246 | 3.26×102 | 1.33×10-4 | 2.02×10-5 | -18.6 |
|  |  |  | 80 | 0.301 | 1.99×102 | 8.97×10-5 | 2.07×10-5 | -14.2 |
|  |  |  | 100 | 0.329 | 1.70×102 | 7.17×10-5 | 2.28×10-5 | -11.8 |
|  |  |  | 120 | 0.295 | 1.30×102 | 6.87×10-5 | 2.22×10-5 | -14.5 |
|  | Acetone |  | 50 | 0.329 | 3.75×100 | 1.62×10-3 | 2.70×10-4 | -142 |
|  |  |  | 80 | 0.443 | 3.47×100 | 1.48×10-3 | 2.92×10-4 | -149 |
|  |  |  | 100 | 0.512 | 3.48×100 | 1.29×10-3 | 3.03×10-4 | -143 |
|  |  |  | 120 | 0.608 | 3.88×100 | 1.14×10-3 | 2.90×10-4 | -133 |
|  | Recovery |  | 50 | 0.140 | 3.12×102 | 4.86×10-5 | 1.83×10-5 | -5.79 |
|  |  |  | 80 | 0.173 | 2.37×102 | 3.34×10-5 | 1.97×10-5 | -2.28 |
|  |  |  | 100 | 0.201 | 3.72×102 | 2.96×10-5 | 1.85×10-5 | -1.67 |
|  |  |  | 120 | 0.211 | 4.05×102 | 2.66×10-5 | 1.85×10-5 | -2.07 |
| 350 | As prepared |  | 50 | 0.0685 | 1.80×102 | 3.83×10-5 | 1.09×10-5 | -19.0 |
|  |  |  | 80 | 0.0902 | 1.12×102 | 2.36×10-5 | 1.00×10-5 | -10.4 |
|  |  |  | 100 | 0.0802 | 8.83×101 | 1.59×10-5 | 8.91×10-6 | -8.36 |
|  |  |  | 120 | 0.0603 | 4.09×101 | 9.97×10-6 | 9.89×10-6 | -7.25 |
|  | Acetone |  | 50 | 0.153 | 6.00×100 | 4.15×10-4 | 8.37×10-5 | -94.6 |
|  |  |  | 80 | 0.303 | 6.31×100 | 4.67×10-4 | 1.15×10-4 | -87.8 |
|  |  |  | 100 | 0.330 | 6.15×100 | 4.15×10-4 | 1.25×10-4 | -89.2 |
|  |  |  | 120 | 0.326 | 5.66×100 | 3.53×10-4 | 1.29×10-4 | -91.2 |
|  | Recovery |  | 50 | 0.0677 | 8.48×102 | 3.12×10-5 | 8.47×10-6 | -12.8 |
|  |  |  | 80 | 0.0730 | 1.31×102 | 1.51×10-5 | 6.99×10-6 | -3.87 |
|  |  |  | 100 | 0.0749 | 9.02×102 | 1.10×10-5 | 7.52×10-6 | -0.799 |
|  |  |  | 120 | 0.0590 | 1.09×103 | 6.87×10-5 | 6.47×10-6 | -0.823 |