Supplementary Information

The role of TiN particles in enhancing the microstructure, tensile, and wear behavior of stir-cast AA7075-Zn alloy composites

Oluwasegun Faloduna,b*, Chidera Onwurahc, Victor Iyamuc, Abiodun Bayodeb

aDepartment of Materials and Metallurgical Engineering, University of Ilorin, Ilorin, Nigeria

bDepartment of Mechanical Engineering, North-West University, Potchefstroom, South Africa

cDepartment of Mechanical Engineering, Covenant University, Ota, Nigeria

*Corresponding author: oefalodun@gmail.com

Figure S1. Transmission electron microscope micrograph of titanium nitride (TiN) powder.

Figure S2. Microhardness of AA7075-Zn alloy strengthened with titanium nitride powder.

Figure S3. X-ray diffraction pattern of AA7075-Zn matrix composites.

Table S1: Chemical composition of AA7075 alloy

| Elements | Al | Si | Mg | Mn | Cu | Fe | Cr | Zn | Ti |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| percentage (wt%) | Bal | 0.42 | 2.21 | 0.29 | 1.50 | 0.47 | 0.21 | 5.23 | 0.24 |

Table S2: Chemical composition of titanium nitride powder

| Elements | C | Si | Ni | N | Ti | Fe |
| --- | --- | --- | --- | --- | --- | --- |
| percentage (wt%) | 0.03 | <0.003 | <0.001 | 21.91 | 77.83 | <0.001 |