Supplemetary Information for paper

Chemical structure analysis of chitosan-modified road bitumen after de-icing salt treatment

Szymon Malinowskia*

*aDepartment of Construction Materials Engineering and Geoengineering, Lublin University of Technology, 20-618 Lublin, Poland

Table S1. Linear regressions of the relationship between chemical changes in the properties of bitumen and the erosion solution in the form of NaCl

| C [%] | Y | X | Equation | R2 | Y | X | equation | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 7-day erosion process |  |  |  |  |  |  |  |  |
| 5 | IOH | TOC | IOH=0.1869[TOC]-0.014 | R2=0.856 | IOH | ΔpH | IOH=-0.0812[ΔpH]+0.016 | R2=0.002 |
|  | IC=O | TOC | IC=O=-0.011[TOC]+0.039 | R2=0.049 | IC=O | ΔpH | IC=O=-0.4074[ΔpH]+0.076 | R2=0.827 |
|  | IC-OH | TOC | IC-OH=1.3873[TOC]+0.978 | R2=0.032 | IC-OH | ΔpH | IC-OH=23.183[ΔpH]+0.885 | R2=0.110 |
|  | ICH2-OH | TOC | ICH2-OH=0.0062[TOC]+0.001 | R2=0.439 | ICH2-OH | ΔpH | ICH2-OH=0.0404[ΔpH]+0.0011 | R2=0.223 |
|  | IC-Cl | TOC | IC-Cl=0.0277[TOC]+0.001 | R2=0.719 | IC-Cl | ΔpH | IC-Cl=0.1777[ΔpH]+0.003 | R2=0.361 |
| 10 | IOH | TOC | IOH=0.0289[TOC]+0.013 | R2=0.013 | IOH | ΔpH | IOH=1.0313[ΔpH]+0.048 | R2=0.151 |
|  | IC=O | TOC | IC=O=0.0312[TOC]-0.0026 | R2=0.297 | IC=O | ΔpH | IC=O=-0.395[ΔpH]+0.0084 | R2=0.465 |
|  | IC-OH | TOC | IC-OH=3.2197[TOC]+2.0431 | R2=0.022 | IC-OH | ΔpH | IC-OH=12.316[ΔpH]+2.475 | R2=0.003 |
|  | ICH2-OH | TOC | ICH2-OH=0.0128[TOC]-0.0006 | R2=0.455 | ICH2-OH | ΔpH | ICH2-OH=-0.096[ΔpH]+0.0031 | R2=0.250 |
|  | IC-Cl | TOC | IC-Cl=-0.0153[TOC]+0.0089 | R2=0.371 | IC-Cl | ΔpH | IC-Cl=0.0713[ΔpH]+0.0052 | R2=0.079 |
| 15 | IOH | TOC | IOH=0.0239[TOC]+0.021 | R2=0.097 | IOH | ΔpH | IOH=-0.952[ΔpH]+0.0363 | R2=0.656 |
|  | IC=O | TOC | IC=O=0.0074[TOC]+0.0051 | R2=0.032 | IC=O | ΔpH | IC=O=-0.461[ΔpH]+0.0122 | R2=0.519 |
|  | IC-OH | TOC | IC-OH=-1.6269[TOC]+1.5603 | R2=0.055 | IC-OH | ΔpH | IC-OH=15.603[ΔpH]+1.142 | R2=0.021 |
|  | ICH2-OH | TOC | ICH2-OH=0.0079[TOC]-0.0001 | R2=0.108 | ICH2-OH | ΔpH | ICH2-OH=-0.248[ΔpH]+0.0044 | R2=0.449 |
|  | IC-Cl | TOC | IC-Cl=-0.001[TOC]+0.0037 | R2=0.007 | IC-Cl | ΔpH | IC-Cl=-0.0519[ΔpH]+0.0042 | R2=0.075 |
| 28-day erosion process |  |  |  |  |  |  |  |  |
| 5 | IOH | TOC | IOH=0.0612[TOC]+0.016 | R2=0.472 | IOH | ΔpH | IOH=0.00003[ΔpH]+0.0192 | R2=0.011 |
|  | IC=O | TOC | IC=O=-0.0614[TOC]+0.0086 | R2=515 | IC=O | ΔpH | IC=O=-0.000006[ΔpH]+0.006 | R2=0.037 |
|  | IC-OH | TOC | IC-OH=-48.055[TOC]+9.980 | R2=0.834 | IC-OH | ΔpH | IC-OH=0.1142[ΔpH]+4.0402 | R2=0.399 |
|  | ICH2-OH | TOC | ICH2-OH=-0.0047[TOC]-0.0025 | R2=0.053 | ICH2-OH | ΔpH | ICH2-OH=0.00002[ΔpH]+0.0017 | R2=0.079 |
|  | IC-Cl | TOC | IC-Cl=0.0086[TOC]+0.0051 | R2=0.322 | IC-Cl | ΔpH | IC-Cl=-0.00002[ΔpH]+0.0053 | R2=0.084 |
| 10 | IOH | TOC | IOH=-0.1796[TOC]+0.037 | R2=0.409 | IOH | ΔpH | IOH=-0.0003[ΔpH]+0.028 | R2=0.493 |
|  | IC=O | TOC | IC=O=0.0074[TOC]+0.0068 | R2=0.006 | IC=O | ΔpH | IC=O=-0.00008[ΔpH]+0.0085 | R2=0.261 |
|  | IC-OH | TOC | IC-OH=40.852[TOC]+2.5962 | R2=0.040 | IC-OH | ΔpH | IC-OH=0.2002[ΔpH]+2.740 | R2=0.414 |
|  | ICH2-OH | TOC | ICH2-OH=0.012[TOC]+0.00001 | R2=0.055 | ICH2-OH | ΔpH | ICH2-OH=0.00006[ΔpH]-0.000009 | R2=0.634 |
|  | IC-Cl | TOC | IC-Cl=-0.0166[TOC]+0.0061 | R2=0.116 | IC-Cl | ΔpH | IC-Cl=-0.00006[ΔpH]+0.0057 | R2=0.613 |
| 15 | IOH | TOC | IOH=0.0257[TOC]+0.0193 | R2=0.1348 | IOH | ΔpH | IOH=0.0004[ΔpH]+0.084 | R2=0.630 |
|  | IC=O | TOC | IC=O=-0.0138[TOC]+0.0071 | R2=0.083 | IC=O | ΔpH | IC=O=0.0002[ΔpH]-0.0002 | R2=0.261 |
|  | IC-OH | TOC | IC-OH=9.911 [TOC]+3.548 | R2=0.021 | IC-OH | ΔpH | IC-OH=0.166[ΔpH]-1.079 | R2=0.120 |
|  | ICH2-OH | TOC | ICH2-OH=0.002[TOC]+0.001 | R2=0.086 | ICH2-OH | ΔpH | ICH2-OH=0.00004[ΔpH]-0.0002 | R2=0.737 |
|  | IC-Cl | TOC | IC-Cl=-0.0002[TOC]+0.0052 | R2=0.0002 | IC-Cl | ΔpH | IC-Cl=-0.00003[ΔpH]+0.0064 | R2=0.124 |

Table S2. Linear regressions of the relationship between chemical changes in the properties of bitumen and the erosion solution in the form of MgCl2

| C [%] | Y | X | Equation | R2 | Y | X | equation | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 7-day erosion process |  |  |  |  |  |  |  |  |
| 5 | IOH | TOC | IOH=-0.3142[TOC]+0.2053 | R2=0.084 | IOH | ΔpH | IOH=-0.0015[ΔpH]+0.092 | R2=0.200 |
|  | IC=O | TOC | IC=O=-0.0157[TOC]+0.0091 | R2=0.319 | IC=O | ΔpH | IC=O=-0.00002[ΔpH]+0.0021 | R2=0.034 |
|  | IC-OH | TOC | IC-OH=11.43[TOC]-2.901 | R2=0.097 | IC-OH | ΔpH | IC-OH=0.0404[ΔpH]+1.569 | R2=0.126 |
|  | ICH2-OH | TOC | ICH2-OH=-0.0122[TOC]+0.0082 | R2=0.027 | ICH2-OH | ΔpH | ICH2-OH=-0.00002[ΔpH]+0.0028 | R2=0.004 |
|  | IC-Cl | TOC | IC-Cl=0.0037[TOC]+0.0032 | R2=0.034 | IC-Cl | ΔpH | IC-Cl=0.00003[ΔpH]+0.0043 | R2=0.221 |
| 10 | IOH | TOC | IOH=-0.2458[TOC]+0.282 | R2=0.270 | IOH | ΔpH | IOH=-0.0111[ΔpH]+0.2209 | R2=0.959 |
|  | IC=O | TOC | IC=O=0.0037[TOC]-0.0015 | R2=0.484 | IC=O | ΔpH | IC=O=0.0001[ΔpH]+0.000006 | R2=0.922 |
|  | IC-OH | TOC | IC-OH=7.827[TOC]-3.258 | R2=0.644 | IC-OH | ΔpH | IC-OH=0.2047[ΔpH]+0.5551 | R2=0.771 |
|  | ICH2-OH | TOC | ICH2-OH=-0.0028[TOC]+0.0035 | R2=0.375 | ICH2-OH | ΔpH | ICH2-OH=0.00002 [ΔpH]+0.001 | R2=0.020 |
|  | IC-Cl | TOC | IC-Cl=-0.0016[TOC]+0.0054 | R2=0.031 | IC-Cl | ΔpH | IC-Cl=0.00002[ΔpH]+0.0039 | R2=0.008 |
| 15 | IOH | TOC | IOH=-0.3388[TOC]+0.0357 | R2=0.751 | IOH | ΔpH | IOH=0.0004[ΔpH]+0.1309 | R2=0.011 |
|  | IC=O | TOC | IC=O=0.0052[TOC]-0.0016 | R2=0.750 | IC=O | ΔpH | IC=O=-0.00004[ΔpH]+0.0022 | R2=0.353 |
|  | IC-OH | TOC | IC-OH=9.5713[TOC]-2.636 | R2=0.236 | IC-OH | ΔpH | IC-OH=0.0201[ΔpH]+3.354 | R2=0.011 |
|  | ICH2-OH | TOC | ICH2-OH=0.0055[TOC]-0.0017 | R2=0.671 | ICH2-OH | ΔpH | ICH2-OH=-0.00005[ΔpH]+0.0025 | R2=0.559 |
|  | IC-Cl | TOC | IC-Cl=-0.0008[TOC]+0.0046 | R2=0.004 | IC-Cl | ΔpH | IC-Cl=0.00009[ΔpH]+0.003 | R2=0.484 |
| 28-day erosion process |  |  |  |  |  |  |  |  |
| 5 | IOH | TOC | IOH=-0.0952[TOC]+0.0366 | R2=0.512 | IOH | ΔpH | IOH=-0.0013[ΔpH]+0.0537 | R2=0.413 |
|  | IC=O | TOC | IC=O=-0.0011[TOC]+0.0051 | R2=0.002 | IC=O | ΔpH | IC=O=0.00006[ΔpH]+0.0039 | R2=0.025 |
|  | IC-OH | TOC | IC-OH=-6.2337[TOC]+3.153 | R2=0.337 | IC-OH | ΔpH | IC-OH=-0.0215[ΔpH]+2.9528 | R2=0.019 |
|  | ICH2-OH | TOC | ICH2-OH=-0.00009[TOC]-0.0019 | R2=0.000008 | ICH2-OH | ΔpH | ICH2-OH=-0.0002[ΔpH]+0.0062 | R2=0.174 |
|  | IC-Cl | TOC | IC-Cl=-0.0014[TOC]+0.0056 | R2=0.080 | IC-Cl | ΔpH | IC-Cl=-0.00005[ΔpH]+0.0065 | R2=0.400 |
| 10 | IOH | TOC | IOH=-0.0642[TOC]+0.0562 | R2=0.428 | IOH | ΔpH | IOH=-0.0023[ΔpH]+0.0645 | R2=0.208 |
|  | IC=O | TOC | IC=O=-0.0097[TOC]+0.0078 | R2=0.336 | IC=O | ΔpH | IC=O=0.0004[ΔpH]-0.0016 | R2=0.171 |
|  | IC-OH | TOC | IC-OH=11.363[TOC]+2.3363 | R2=0.555 | IC-OH | ΔpH | IC-OH=-0.63[ΔpH]+16.44 | R2=0.630 |
|  | ICH2-OH | TOC | ICH2-OH=-0.0208[TOC]+0.0097 | R2=0.942 | ICH2-OH | ΔpH | ICH2-OH=0.0006[ΔpH]-0.0071 | R2=0.2439 |
|  | IC-Cl | TOC | IC-Cl=0.0051[TOC]+0.0035 | R2=0.440 | IC-Cl | ΔpH | IC-Cl=0.00005[ΔpH]+0.0048 | R2=0.016 |
| 15 | IOH | TOC | IOH=0.0493[TOC]+0.0067 | R2=0.043 | IOH | ΔpH | IOH=-0.0012[ΔpH]+0.0448 | R2=0.031 |
|  | IC=O | TOC | IC=O=-0.0315[TOC]+0.0172 | R2=0.442 | IC=O | ΔpH | IC=O=0.0002[ΔpH]+0.00006 | R2=0.032 |
|  | IC-OH | TOC | IC-OH=61.216[TOC]-23.525 | R2=0.714 | IC-OH | ΔpH | IC-OH=0.0786[ΔpH]+2.3924 | R2=0.002 |
|  | ICH2-OH | TOC | ICH2-OH=0.0038[TOC]-0.0009 | R2=0.291 | ICH2-OH | ΔpH | ICH2-OH=-0.00009[ΔpH]+0.002 | R2=0.186 |
|  | IC-Cl | TOC | IC-Cl=-0.0106[TOC]+0.0099 | R2=0.113 | IC-Cl | ΔpH | IC-Cl=-0.0003[ΔpH]+0.0017 | R2=0.084 |

Table S3. Linear regressions of the relationship between chemical changes in the properties of bitumen and the erosion solution in the form of CaCl2

| C [%] | Y | X | Equation | R2 | Y | X | equation | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 7-day erosion process |  |  |  |  |  |  |  |  |
| 5 | IOH | TOC | IOH=-0.8558[TOC]+0.1992 | R2=0.806 | IOH | ΔpH | IOH=-0.0025[ΔpH]+0.3079 | R2=0.620 |
|  | IC=O | TOC | IC=O=0.0231[TOC]-0.0028 | R2=0.550 | IC=O | ΔpH | IC=O=0.0001[ΔpH]-0.009 | R2=0.899 |
|  | IC-OH | TOC | IC-OH=-3.4944[TOC]+0.9019 | R2=0.330 | IC-OH | ΔpH | IC-OH=-0.0048[ΔpH]+0.772 | R2=0.056 |
|  | ICH2-OH | TOC | ICH2-OH=0.052[TOC]+0.034 | R2=0.007 | ICH2-OH | ΔpH | ICH2-OH=-0.00003[ΔpH]+0.0073 | R2=0.017 |
|  | IC-Cl | TOC | IC-Cl=0.0189[TOC]+0.0012 | R2=0.414 | IC-Cl | ΔpH | IC-Cl=0.00008[ΔpH]-0.0041 | R2=0.722 |
| 10 | IOH | TOC | IOH=-0.209[TOC]+0.07 | R2=0.023 | IOH | ΔpH | IOH=-0.0017[ΔpH]+0.2107 | R2=0.293 |
|  | IC=O | TOC | IC=O=0.0216[TOC]-0.0026 | R2=0.395 | IC=O | ΔpH | IC=O=0.00005[ΔpH]-0.0035 | R2=0.395 |
|  | IC-OH | TOC | IC-OH=1.2992[TOC]-0.0378 | R2=0.090 | IC-OH | ΔpH | IC-OH=0.0088[ΔpH]-0.7215 | R2=0.790 |
|  | ICH2-OH | TOC | ICH2-OH=-0.0346[TOC]+0.0122 | R2=0.145 | ICH2-OH | ΔpH | ICH2-OH=-0.00003 [ΔpH]+0.0084 | R2=0.023 |
|  | IC-Cl | TOC | IC-Cl=0.0018[TOC]+0.0052 | R2=0.049 | IC-Cl | ΔpH | IC-Cl=-0.00001[ΔpH]+0.0069 | R2=0.436 |
| 15 | IOH | TOC | IOH=-0.6313[TOC]+0.169 | R2=0.307 | IOH | ΔpH | IOH=-0.0041[ΔpH]+0.4711 | R2=0.312 |
|  | IC=O | TOC | IC=O=0.0152[TOC]-0.0014 | R2=0.520 | IC=O | ΔpH | IC=O=0.00005[ΔpH]-0.0034 | R2=0.123 |
|  | IC-OH | TOC | IC-OH=6.992[TOC]-0.6175 | R2=0.604 | IC-OH | ΔpH | IC-OH=0.0479[ΔpH]-4.2052 | R2=0.679 |
|  | ICH2-OH | TOC | ICH2-OH=-0.0022[TOC]+0.0032 | R2=0.001 | ICH2-OH | ΔpH | ICH2-OH=-0.00002[ΔpH]+0.0191 | R2=0.087 |
|  | IC-Cl | TOC | IC-Cl=0.0007[TOC]+0.0053 | R2=0.005 | IC-Cl | ΔpH | IC-Cl=-0.00002[ΔpH]+0.0077 | R2=0.128 |
| 28-day erosion process |  |  |  |  |  |  |  |  |
| 5 | IOH | TOC | IOH=-0.1958[TOC]+0.0437 | R2=0.626 | IOH | ΔpH | IOH=-0.0001[ΔpH]+0.0431 | R2=0.024 |
|  | IC=O | TOC | IC=O=0.0237[TOC]+0.0031 | R2=0.101 | IC=O | ΔpH | IC=O=0.0001[ΔpH]-0.0069 | R2=0.248 |
|  | IC-OH | TOC | IC-OH=8.4069[TOC]-0.162 | R2=0.532 | IC-OH | ΔpH | IC-OH=0.0005[ΔpH]+0.3338 | R2=0.0001 |
|  | ICH2-OH | TOC | ICH2-OH=-0.0138[TOC]+0.002 | R2=0.247 | ICH2-OH | ΔpH | ICH2-OH=-0.00004[ΔpH]+0.0053 | R2=0.231 |
|  | IC-Cl | TOC | IC-Cl=0.00003[TOC]+0.0053 | R2=0.00005 | IC-Cl | ΔpH | IC-Cl=-0.00002[ΔpH]+0.0073 | R2=0.328 |
| 10 | IOH | TOC | IOH=0.0622[TOC]+0.0121 | R2=0.082 | IOH | ΔpH | IOH=0.00007[ΔpH]+0.0023 | R2=0.025 |
|  | IC=O | TOC | IC=O=-0.0695[TOC]+0.03 | R2=0.595 | IC=O | ΔpH | IC=O==-0.0001[ΔpH]+0.0248 | R2=0.600 |
|  | IC-OH | TOC | IC-OH=3.3878[TOC]-0.9177 | R2=0.831 | IC-OH | ΔpH | IC-OH=0.0026[ΔpH]-0.1872 | R2=0.112 |
|  | ICH2-OH | TOC | ICH2-OH=0.1273[TOC]-0.0338 | R2=0.582 | ICH2-OH | ΔpH | ICH2-OH=0.0002[ΔpH]-0.0129 | R2=0.210 |
|  | IC-Cl | TOC | IC-Cl=-0.0146[TOC]+0.0094 | R2=0.530 | IC-Cl | ΔpH | IC-Cl=-0.00002[ΔpH]+0.0068 | R2=0.141 |
| 15 | IOH | TOC | IOH=0.4629[TOC]-0.1669 | R2=0.810 | IOH | ΔpH | IOH=0.0008[ΔpH]-0.0578 | R2=0.366 |
|  | IC=O | TOC | IC=O=0.0644[TOC]-0.0235 | R2=0.789 | IC=O | ΔpH | IC=O=0.0002[ΔpH]-0.0138 | R2=0.797 |
|  | IC-OH | TOC | IC-OH=12.056[TOC]-4.6036 | R2=0.794 | IC-OH | ΔpH | IC-OH=0.0159[ΔpH]-1.3187 | R2=0.222 |
|  | ICH2-OH | TOC | ICH2-OH=0.0549[TOC]-0.0202 | R2=0.862 | ICH2-OH | ΔpH | ICH2-OH=0.0009[ΔpH]-0.0091 | R2=0.554 |
|  | IC-Cl | TOC | IC-Cl=-0.0225[TOC]+0.0147 | R2=0.728 | IC-Cl | ΔpH | IC-Cl=-0.00004[ΔpH]+0.0095 | R2=0.348 |