Supplementary Material: Composition-Structure Relationships for Calcium Aluminosilicate Glasses

Subhashree Panda1, Meili Liu1, Rudra N. Purusottam2,3, Jamie D. Walls3, Luis Ruiz Pestana1, Prannoy Suraneni1*

1Civil and Architectural Engineering, University of Miami, Coral Gables, FL 33146

2School of Chemistry and Chemical Engineering, Queen’s University Belfast, Belfast, United Kingdom BT9 5AG

3Department of Chemistry, University of Miami, Coral Gables, FL 33146

*Corresponding author: Prannoy Suraneni, suranenip@miami.edu

Figure S1. Ratio of non-bridging oxygen to oxygen in a tetragonal coordination ratio (NBO/T) plotted against CaO content. The NBO/T values were calculated from MD simulations [1].

Table S1. The isotropic chemical shifts at the spectral maximum of 29Si and the various oxidation states of 27Al in the CAS glasses.

| Glass | 29Si (ppm) | [AlO4] (ppm) | [AlO5] (ppm) | [AlO6] (ppm) |
| --- | --- | --- | --- | --- |
| C65A20S15 | -73 | 73 | 47 | 19 |
| C53A35S12 | -72 | 72 | 30 | 5 |
| C50A30S20 | -75 | 71.5 | 29 | 5 |
| C40A10S50 | -80 | 66 | 37 | 11 |
| C33A33S33 | -79 | 62 | 36 | 9 |
| C30A50S20 | -78 | 60 | 33 | 9 |
| C21A18S61 | -87 | 59 | - | - |
| C10A10S80 | -108 | 51 | 18 | - |

Figure S2. The fraction of Si(Qn) calculated from MD simulations [1] plotted against CaO.

Figure S3. The fraction of Al(Qn) calculated from MD simulations [1] plotted against CaO.

Figure S4. Average (Al)Qn species calculated from MD simulations [1] plotted against the 27Al NMR isotropic shift at the spectral maximum.

Figure S5. FTIR spectra of the CAS glasses.

Figure S6. Band 1 maxima location plotted against (a) ∠Al-O-Al; (b) ∠Si-O-Al; (c) ∠Si-O-Si.

T-O-T’ angles were calculated from MD simulations [1].

Figure S7. (a) XRD hump maxima angle plotted against SiO2; (b) 29Si NMR isotropic shift at the spectral maximum plotted against SiO2; (c) 27Al NMR isotropic shift at the spectral maximum plotted against SiO2.

Figure S8. (a) XRD hump maxima angle plotted against Al2O3; (b) 29Si NMR isotropic shift at the spectral maximum plotted against Al2O3; (c) 27Al NMR isotropic shift at the spectral maximum plotted against Al2O3.

References

- Liu, M., Panda, S., Suraneni, P. and Pestana, L.R., 2023. Insights from molecular dynamics into the chemistry-structure relationships of calcium aluminosilicate glasses. Journal of Non-Crystalline Solids, 618, p.122545. https://doi.org/10.1016/j.jnoncrysol.2023.122545