Reactivity and Reaction Kinetics of Calcium Aluminosilicate Glasses

Subhashree Panda1, Luis Ruiz Pestana1, Prannoy Suraneni1

1Civil and Architectural Engineering, University of Miami, Coral Gables, Florida 33146

*Corresponding author: Prannoy Suraneni, suranenip@miami.edu

Table S1. X-ray fluorescence oxide contents for selected compositions.

| Compositions | Weight% |  |  |
| --- | --- | --- | --- |
|  | CaO | Al2O3 | SiO2 |
| C65A20S12 | 67.4 | 19.2 | 15.2 |
| C53A35S12 | 50.2 | 39.4 | 11.3 |
| C50A30S20 | 52.5 | 27.4 | 20.7 |
| C40A10S50 | 37.4 | 13.3 | 48.4 |
| C33A33S33 | 35.5 | 29.8 | 35.4 |
| C30A50S20 | 30.4 | 51.8 | 22.6 |
| C21A18S61 | 19.4 | 19.2 | 60.7 |
| C10A10S80 | 10.5 | 11.2 | 83.1 |

Figure S1. (a) Differential PSD data; (b) Cumulative PSD data of the synthesized CAS glasses.

Figure S2. SEM images of (a) C63A20S15 glass; (b) C30A50S20 glass.

Figure S3. (a) Heat release normalized to SCM specific surface area plotted against time; (b) Heat release normalized to SCM specific surface area plotted against heat release normalized to SCM mass.

Figure S4. H72 plotted against (a) SiO2; (b) Al2O3 with Ca/Si ratio in colormap.

Figure S5. H12 plotted against (a) CaO; (b) CaO/SiO2; (c) SiO2; (d) Al2O3.

Figure S5. H12 plotted against (a) CaO; (b) CaO/SiO2; (c) SiO2; (d) Al2O3 with Ca/Si ratio in colormap.

Figure S6. H72/H12 plotted against (a) SiO2; (b) Al2O3.

Table S2. Band maxima locations for various bands obtained from FTIR deconvolution.

| Composition | Bending vibration T-O-T’ | Symmetric stretching vibration T-O-T’ | Q1 (Si) | Q2 (Si) | Q3 (Si) | Q4 (Si) |
| --- | --- | --- | --- | --- | --- | --- |
| C65A20S15 | 653 | 779 | 850 | 935 | - | - |
| C53A35S12 | 653 | 782 | 860 | 965 | - | - |
| C50A30S20 | 658 | 790 | 890 | 990 | - | - |
| C45A35S20 | 658 | 795 | 874 | 972 | - | - |
| C40A40S20 | 658 | 792 | 865 | 974 | - | - |
| C40A30S30 | 662 | 799 | 860 | 967 | - | - |
| C40A20S40 | 661 | - | 856 | 939 | 1021 | - |
| C40A10S50 | 672 | - | 855 | 950 | 1035 | 1115 |
| C35A45S20 | 663 | 797 | 858 | 964 | - | - |
| C33A33S33 | 673 | 808 | 895 | 993 | 1085 | - |
| C30A50S20 | 662 | 805 | 885 | 998 | - | - |
| C30A30S40 | 664 | - | 873 | 958 | 1075 | - |
| C25A25S50 | 667 | - | 899 | 953 | 1062 | 1161 |
| C21A18S61 | 685 | - | 897 | 948 | 1045 | 1155 |
| C20A30S50 | 669 | - | 896 | 957 | 1068 | 1163 |
| C10A10S80 | 695 | 799 | - | 952 | 1080 | 1202 |

Figure S7. The deconvoluted FTIR spectra of the CAS glasses.

Figure S8. (a) XRD hump maxima angle plotted against SiO2; (b) NBO/T plotted against SiO2 [1]; (c) Metal-oxygen bond strength (SM-O) plotted against SiO2 [2]; (d) Topological constraint parameter plotted against SiO2 [3].

Figure S9. (a) XRD hump maxima angle plotted against Al2O3; (b) NBO/T plotted against Al2O3 [1]; (c) Metal-oxygen bond strength (SM-O) plotted against Al2O3 [2]; (d) Topological constraint parameter plotted against Al2O3 [3]. Ca/Si ratio is plotted in the colormap.

Figure S10. H72/H12 plotted against (a) XRD hump maxima angle; (b) NBO/T [1]; (c) Average Qn [1]; (d) Metal-oxygen bond strength (SM-O) [2]; (e) Topological constraint parameter [3]. The linear fit only includes the solid points, as the two hollow points (C65A20S15 and C53A35S12) show low values of H12 and H72, and the H72/H12 values are likely unreliable.

References

- Liu, M., Panda, S., Suraneni, P. and Pestana, L.R., 2023. Insights from molecular dynamics into the chemistry-structure relationships of calcium aluminosilicate glasses. Journal of Non-Crystalline Solids, 618, p.122545. https://doi.org/10.1016/j.jnoncrysol.2023.122545

- Gong, K. and Olivetti, E.A., 2022. Development of structural descriptors to predict dissolution rate of volcanic glasses: Molecular dynamic simulations. Journal of the American Ceramic Society, 105(4), pp.2575-2594. https://doi.org/10.1111/jace.18265

- Gong, K. and White, C.E., 2023. Development of physics-based compositional parameters for predicting the reactivity of amorphous aluminosilicates in alkaline environments. Cement and Concrete Research, 174, p.107296. https://doi.org/10.1016/j.cemconres.2023.107296