Supplementary Material

Fig S1. XRD plots before and after MCA for a. BA and BF, b. CL and DS.

Fig. S2a. TGA and differential thermogravimetric analyses (DTG) for DS and DS-60, b. TGA and DTG of DS and DS-60 (25 °C to 300 °C).

Fig S3. R3 test heat release over time.

Fig. S4a. R3 test H168 as a function of the modified R3 test H72, b. R3 test H168 as a function of AC.

Fig. S5. Compressive strength as a function of bulk resistivity.

Table S1. H∞ values of the different systems.

| System | 7-day heat release (J/g) | H∞ (J/g) |
| --- | --- | --- |
| PLC | 295 | 406 |
| BA | 210 | 255 |
| BA-60 | 266 | 358 |
| BF | 227 | 294 |
| BF-60 | 257 | 369 |
| CL | 233 | 296 |
| CL-60 | 254 | 348 |
| DS | 234 | 280 |
| DS-60 | 264 | 348 |