# Supporting Information

Toward continuous shrinkage measurement of poured earth: practical setup and underlying shrinking mechanisms

Yi Du1,2*, Ellina Bernard1,2, Janis Justs1, Guillaume Habert2, Pietro Lura1,3

1Empa, Swiss Federal Laboratories for Materials Science and Technology, Laboratory for Concrete and Asphalt, Dübendorf CH-8600, Switzerland

2Institute of Construction and Infrastructure Management, Chair of Sustainable Construction, Swiss Federal Institute of Technology (ETH Zurich), Zurich CH-8093, Switzerland

3Institute for Building Materials, ETH Zurich, Swiss Federal Institute of Technology (ETH Zurich), Zurich CH-8093, Switzerland

*Correspondence: yi.du@empa.ch

Fig. S1. Gravimetric water content evolution of prismatic and semi-cylindrical samples following drying. Note that the water content was calculated based on the mass loss curves.

Table S1. Duration, mass loss, and water content of the CRP stage for prismatic and semi-cylindrical samples during drying

| Sample | CRP stage |  |
| --- | --- | --- |
| Prismatic Sample | Duration, h | 5.5-6 |
|  | Mass loss, kg/m2 | 5.7 ~ 6.0 |
|  | Water content | 0.12-0.115 |
| Semi-Cyl. Sample | Duration, h | 4-5 |
|  | Mass loss, kg/m2 | 4.7-5.7 |
|  | Water content | 0.12-0.11 |

Fig. S2. Mass loss of square samples with different thicknesses over drying time.

Fig. S3. Vertical deformation of square and semi-cylindrical sample measured by DIC as a function of mass loss. The dashed line represents the bleeding settlement calculated from mass loss.